Concrete Solutions® Concrete Overlays – Repair Guide Specification

Note: These specifications were current at the time of publication but are subject to change without notice. Please confirm the accuracy of these specifications with the manufacturer and / or distributor prior to installation. Specification writer shall choose the most appropriate section that applies to a given scope of work.

SECTION 03 01 50 MAINTENANCE OF CAST DECKS AND UNDERLAYMENT

SECTION 03 35 39 SPRAYABLE CEMENTITIOUS OVERLAY

SECTION 03 53 00 CONCRETE TOPPING

SECTION 09 97 26 CEMENTITIOUS COATINGS

SECTION 32 01 26 RIGID PAVING REHABILITATION

SECTION 32 13 16 DECORATIVE CONCRETE PAVING

SPECIFIER NOTE:  This product guide specification is written according to the Construction Specifications Institute (CSI) Format, including MasterFormat, SectionFormat, and PageFormat, as contained in the CSI Manual of Practice.

This section must be carefully reviewed and edited by the Architect to meet the requirements of the project and local building codes. Coordinate this section with other specification sections drawings.

This guide specification is intended to be used by a qualified construction specifier. It should not be used without appropriate modifications.  Notes for review by specifier begin with “SPECIFIER NOTE.” Optional text requiring a selection is enclosed within brackets, e.g., “Color shall be [white] [tan].” Items requiring specifier input are indicated by a blank line enclosed within brackets, e.g., “Color: [_______].” Delete all italicized “Specifier Notes” and non-applicable optional text in final specification.

This section is based on systems manufactured by Rhino Linings Corporation, 9747 Businespark Avenue, San Diego, CA 92131 Telephone: 1-800-422-2603, FAX 858-450-6881, www.concretesolutions.com.  For assistance with specific product applications, please contact the manufacturer.   Contact the manufacturer for additional information and for assistance in editing this section for your specific application.

PART 1:   GENERAL

  - Section Includes

SPECIFIER NOTE:  Edit the following list as required for the project. Delete optional text below for exterior concrete pavement or interior concrete floor that is not required.

- Overlay cementitious toppings for resurfacing concrete [pavement] [floor].

1.2   Related Sections

SPECIFIER NOTE:  Edit the following list of related sections as required for the project. List other sections with work directly related to this section as required.

- Section 32 13 13 – Concrete Paving (for cast-in-place concrete pavement with overlay cementitious toppings)

- Section 03 30 00 - Cast-In-Place Concrete  (for interior concrete with overlay cementitious toppings)

1.3  Submittals

- Submit according to Section 01 33 00 - Submittal Procedures.

- Product Data: For each product indicated submit manufacturer's product data, including installation instructions.

- Sample Panels: [2 by 2 feet (610 by 610 mm)] [_______], to demonstrate finish of overlay cementitious topping.

- Qualification Data: For Installer and manufacturer specified in Quality Assurance Article, including names and addresses of completed projects, architects, and owners.

1.4  Quality Assurance

- Manufacturer Qualifications: Company specializing in manufacturing products specified in this section with minimum three years documented experience.

- Installer Qualifications: Minimum two years documented experience with projects of similar scope and quality.

SPECIFIER NOTE:  Delete paragraph above or below.

- Installer Qualifications: Trained or approved by Manufacturer of overlay cementitious topping systems.

- Material Source Limitations:  Obtain products from same source throughout Project.

SPECIFIER NOTE:  For large projects or where color and appearance are critical, include provisions for a field sample to demonstrate range of finishes and workmanship, including curing procedures.  Approved field samples set quality standards for comparison with remaining work.

- Field Samples:  Locate at site and obtain approval before start of final work.

  - Field samples shall be minimum [4 by 4 feet (1.2 by 1.2 m)] [_______].

  - [Remove field samples when directed.] [Approved field samples may become part of the completed Work if undisturbed at completion of project.]

SPECIFIER NOTE:  Delete paragraph below if pre-installation conference is not required.

- Pre-installation Conference: Conduct conference at site to comply with requirements of Section 01 31 19 – Project Meetings.

1.5  Delivery, Storage and Handling

- Comply with manufacturer's recommendations for delivery, storage and handling.

- Deliver materials to site in manufacturer’s original, unopened packaging, with labels clearly identifying product name, manufacturer, and location of installation. Upon delivery, materials shall be inspected for damage. Defective materials shall not be used.

- Storage: Store materials in a clean, dry, indoor area in accordance with manufacturer’s instructions. Keep temporary protective coverings in place.

- Handling: Handle products according to manufacturer’s printed instructions.

1.6  Project Conditions

- Environmental Requirements: Comply with overlay cementitious topping manufacturer's instructions.

  - Concrete substrate temperature and air temperature and recommended to be between 45 to 85 deg F before and during installation. Applications outside of this temperature range require additional precautions.

  - In hot weather, install overlay cementitious topping in early morning or when surfaces are shaded.

  - Keep bagged products out of sunlight. Use cool water; do not use water from hot watering hoses.

  - Protect overlay cementitious topping from rain for 24 hours.

  - In windy weather, protect adjacent construction from over-spray during application of sealers.

PART 2:  PRODUCTS

2.1 Acceptable Manufacturer

- Rhino Linings Corporation, 9747 Businespark Avenue, San Diego, CA 92131   
Phone: 1-800-422-2603, Fax:  858-450-6881 Web: www.concretesolutions.com.

SPECIFIER NOTE:  Delete one of the following two paragraphs; coordinate with requirements of Division 1 on product options and substitutions.

- Substitutions: Not permitted.

- Requests for substitutions will be considered in accordance with provisions of Section 01 60 00.

SPECIFIER NOTE:  Edit the following paragraphs as required for the project.  Delete those not required.

2.2   Overlay Cementitious Topping Materials

- Resurfacer Base Coat: Concrete Solutions Resurfacer made with powder polymer, a mixture of gray or white cement and #60 silica sand.

- Primer: Concrete Solutions MRB Primer over unsealed concrete.

SPECIFIER NOTE: Delete subparagraph below if moisture seepage in the concrete substrate is less than 8 lbs. Delete subparagraph above if moisture seepage in the concrete substrate is over 8 lbs.

B.   Primer: Concrete Solutions Moisture Guard followed by Concrete Solutions MRB primer over unsealed concrete.

- Overlay Cementitious Topping: Polymer-modified cementitious topping designed for resurfacing stable, non-moving concrete [floors] [pavements].

- Product: [Concrete Solutions Spray-Top® Polymer Cement] [Concrete Solutions Trowel-Top™ Polymer Cement] [Concrete Solutions Texture-Top™ Bag Mix] [Concrete Solutions Stamp-Top™]

- Water:  Potable

2.3  Integrally-Colored Overlay Materials

- Concrete Solutions Integral Color Pak: factory-measured powdered mix, consisting of nonfading finely ground synthetic mineral-oxide coloring pigments and water reducing wetting agent.

- Colors: As selected by [Architect] [________].

SPECIFIER NOTE: Delete subparagraph above if colors are selected and indicate Concrete Solutions Integral Color Pack name in subparagraph below. Add a schedule if multiple colors are required. Delete subparagraph below if colors are not selected.

- Color: Concrete Solutions Integral Color Pak [________].

2.4  Sealing Materials

- ASTM C 309, membrane-forming sealing compound: liquid applied, non-yellowing, VOC-compliant, gloss finish when cured.

- Product: [Concrete Solutions Stamped Concrete Sealer, Acrylic Urethane or Sealcoat 1000 for outdoor applications] [Acrylic Urethane or Sealcoat 1000, WB Epoxy or WB Urethane for indoor applications (WB Urethane Color is for use over Texture Top)].

SPECIFIER NOTE: Delete paragraph below if slip-resistive additive is not required for interior concrete.

- Slip-Resistive Additive: [Finely graded aggregate or polymer additive designed to add directly to sealer before application for slip-resistant surface.] [Aluminum Oxide aggregate designed to hand broadcast over the first layer of sealer while tacky for a slip-resistant surface.]

2.5  Mixing

- Mix materials in accurate proportions and according to manufacturer's instructions.

- Bulk Mixing: For machine mixing of overlay cementitious topping, use a paddle mortar mixer.

PART 3:  EXECUTION

3.1 Examination

- Site Verification of Conditions:  Verify installation conditions previously established under other sections are acceptable for product installation in accordance with manufacturer's instructions.

- Examine substrate for compliance with requirements.

- Do not proceed with overlay cementitious topping installation until unacceptable conditions are corrected.

3.2   Substrate Preparation

- Map out locations of existing control joints before installation of overlay cementitious topping.

- Thoroughly clean substrate using high-pressure water or trisodium phosphate (TSP) and water with a scrub brush, then rinse thoroughly. Remove potential bond breakers, such as grease, oil, silicone, paint, sealant, curing and sealing compounds, drywall taping compound, etc.

- For painted, sealed, or overly slick hard-troweled concrete substrates, mechanically abrade surfaces by sanding, scarifying, or shot blasting to allow for proper bonding.

- Remove weak, delaminated, or unsound concrete substrates.

SPECIFIER NOTE: Delete optional text below if concrete does not require patching.

- Patching: Fill chips, pits, small holes and spalls smaller than 1/2 inch prior to application of overlay cementitious topping with the Concrete Solutions Resurfacer. For chips, pits, small holes and spalls that are between 1/2 inch and 2 inches use the Concrete Solutions Patching Mix. For chips, pits, small holes and spalls deeper than 2 inches make a patch mix in accordance with the Concrete Solutions Concrete Polymer Patch Mix - Mixing and Coverage Chart.

- Crack and Joint Repair: Reference the Concrete Solutions Crack Repair Instructions and mend in accordance to that guide based on the size and type of cracks being addressed.

- Allow surfaces to dry thoroughly prior to application of primer.

SPECIFIER NOTE: Delete Article below if priming substrate for added durability is not required.

3.3  Priming Substrates

- Apply the appropriate primer to the surface and allow to dry for 3 hours.

- Apply an even squeegee of the Concrete Solutions Resurfacer less than 1/16” using a special metal edged squeegee or hand trowel. Protect adjacent surfaces from overspray or splash.

- Prevent contamination of primed surfaces by dirt or other deleterious materials or conditions.

- Once surface dries, usually within 4-6 hours, Spray-Top or Trowel-Top can be applied.

SPECIFIER NOTE: Delete Article below if cementitious topping is trowel-applied

.3.4  Spray-Applied Overlay Cementitious Topping Placement

- Application: Use Spray-Top machine to apply cementitious topping to a smooth, uniform finish.

- Strain Spray-Top mixture using a nylon strainer before adding it Spray-Top machine.

- Hold the gun 2-3 feet away from the surface you are spraying.

SPECIFIER NOTE: Delete Article below if cementitious topping is spray-applied

3.5  Trowel-Applied Overlay Cementitious Topping Placement

- Trowel Application: Distribute overlay cementitious topping by trowel or squeegee to provide a smooth uniform surface.

- Clean tools frequently to avoid build up of topping materials.

- Limited amounts of water can be used to aid in workability but should never be allowed to puddle. Retemper overlay cementitious topping may be necessary in hot conditions.

SPECIFIER NOTE: Delete Article below if overlay cementitious topping is indoor or not required.

3.6  Broom Finish

- Apply fine broom finish to overlay cementitious topping immediately following initial troweling of material. Clean broom by hand after each pass.

SPECIFIER NOTE: Delete Article below if trowel finish overlay cementitious topping is not required. Hard trowel finish is not recommended for exterior overlay cementitious topping.

- Trowel Finish: Finish as required to achieve desired surface.

3.7  Joints

- Recut existing control joints before cracking occurs, generally within 12 to 24 hours after placement at 70 degrees Fahrenheit.

SPECIFIER NOTE: Delete optional text below if antiquing color is not required for stamped overlay or if cementitious stampable overlay is stained.

3.8  Sealing

- Sealer Application: Apply uniformly in continuous operation by sprayer or short nap roller according to manufacturer's instructions. After initial application is dry and tack free, apply a second coat.  Do not over apply or apply in a single heavy coat.

SPECIFIER NOTE: Delete subparagraphs below for interior concrete. For interior applications subject to wetting, consider slip-resistant floor wax over sealer.

  - Thoroughly mix slip-resistant additive in sealer according to manufacturer's instructions. Stir occasionally to maintain uniform distribution of additive.

SPECIFIER NOTE: Delete subparagraph below if slip resistant additive is used. Delete subparagraph above if aluminum oxide aggregate is used.

- While the first layer of sealer is still tacky, hand broadcast aluminum oxide    aggregate evenly over the entire surface until coverage is adequate for slip resistance. Apply the second coat of sealer after the initial coat is dry and tack free.

  - Verify adequacy of slip resistance before opening up surfaces to traffic.

3.11  Cleaning, Protection & Repair

- Repair damaged overlay cementitious topping according to manufacturer's instructions.

- Clean spillage and soiling from adjacent construction according to manufacturer's instructions.

- Protect overlay cementitious topping from damage or deterioration until date of Substantial Completion.

- Remove construction debris from project site in accordance with provisions outlined in Division 1.

END OF SECTION