Concrete Solutions® Acid Stain and Concrete Dye Guide Specification

Note: These specifications were current at the time of publication but are subject to change without notice. Please confirm the accuracy of these specifications with the manufacturer and / or distributor prior to installation. Specification writer shall choose the most appropriate section that applies to a given scope of work.

SECTION 03 35 19 COLORED CONCRETE FINISHING

SECTION 03 35 40  CHEMICALLY STAINED CONCRETE

SECTION 32 13 13.25  STAINED CONCRETE PAVING

SPECIFIER NOTE:  This product guide specification is written according to the Construction Specifications Institute (CSI) Format, including MasterFormat, SectionFormat, and PageFormat, as contained in the CSI Manual of Practice.

This section must be carefully reviewed and edited by the Architect to meet the requirements of the project and local building codes. Coordinate this section with other specification sections and drawings.

This guide specification is intended to be used by a qualified construction specifier. It should not be used without appropriate modifications.  Notes for review by specifier begin with “SPECIFIER NOTE.” Optional text requiring a selection is enclosed within brackets, e.g., “Color shall be [white] [tan].” Items requiring specifier input are indicated by a blank line enclosed within brackets, e.g., “Color: [_______].” Delete all italicized “Specifier Notes” and non-applicable optional text in final specification.

This section is based on systems manufactured by Rhino Linings Corporation, 9747 Businesspark Avenue, San Diego, CA 92131 Telephone: 1-800-422-2603, FAX 858-450-6881, www.concretesolutions.com.  For assistance with specific product applications, please contact the manufacturer. Contact the manufacturer for additional information and for assistance in editing this section for your specific application.

PART 1:   GENERAL

  - Section Includes

SPECIFIER NOTE: Edit the following list as required for the project. Delete optional text below for exterior concrete pavement or interior concrete floor that is not required.

- Stained concrete for [pavement] [floor].

- Sealer

1.2   Related Sections

SPECIFIER NOTE:  Edit the following list of related sections as required for the project. List other sections with work directly related to this section as required.

- Section 32 13 13 – Concrete Paving (for stained cast-in-place concrete pavement)

- Section 03 30 00 - Cast-In-Place Concrete  (for interior stained cast-in-place concrete)

- Section 03 53 00 – Stamped Concrete Overlay (for stained cementitious stampable overlays)

- Section 03 01 30 – Stamped Concrete Overlay Resurfacing (for stained overlay cementitious toppings)

1.3  Submittals

- Submit according to Section 01 33 00 - Submittal Procedures.

- Product Data: For each product indicated submit manufacturer's product data, including installation instructions.

- Sample for Initial Selection: Manufacturer’s color charts.

- Qualification Data: For installer and manufacturer specified in Quality Assurance Article, including names and addresses of completed projects, architects, and owners.

1.4  Quality Assurance

- Manufacturer Qualifications: Company specializing in manufacturing products specified in this section with minimum three years documented experience.

- Installer Qualifications: Minimum two years documented experience with projects of similar scope and quality.

SPECIFIER NOTE:  Delete paragraph above or below.

- Installer Qualifications: Trained or approved by manufacturer of stain products.

- Material Source Limitations:  Obtain products from same source throughout project.

SPECIFIER NOTE:  Older concrete, typically exterior concrete exposed to rain or runoff may be weathered beyond the possibility of staining. Determine ability of substrate to react with stain with field samples prior to start of final work. If substrate cannot react with stain, an alternative coloring method is recommended. Approved field samples set quality standards for comparison with remaining work.

- Field Samples:  Locate at site and obtain approval before start of final work. Field samples should demonstrate range of colors, finishes and workmanship, including sealing procedures. If stain does not visibly fizz, additional cleaning is required, or pH of concrete is too low to react with stain.

  - Field samples shall be a minimum [4 by 4 feet (1.2 by 1.2 m)] [_______].

  - [Remove field samples when directed.] [Approved field samples may become part of the completed work if undisturbed at completion of project.]

SPECIFIER NOTE:  Delete paragraph below if pre-installation conference is not required.

- Pre-installation Conference: Conduct conference at site to comply with requirements of Section 01 31 19 – Project Meetings.

1.5  Delivery, Storage and Handling

- Comply with manufacturer's recommendations for delivery, storage and handling.

- Deliver materials to site in manufacturer’s original, unopened packaging, with labels clearly identifying product name, manufacturer, and location of installation. Upon delivery, materials shall be inspected for damage. Defective materials shall not be used.

- Storage: Store materials in a clean, dry indoor area in accordance with manufacturer’s instructions. Keep temporary protective coverings in place.

- Handling: Handle products according to manufacturer’s printed instructions.

1.6  Project Conditions

- Environmental Requirements: Comply with stain manufacturer's instructions.

  - Do not apply stain if concrete substrate temperature is not between 50 to 85 °F before and during installation.

  - Do not apply stain if air temperature is not between 50 and 85 °F during installation, and for at least 48 hours after installation.

  - In hot weather, install stain in early morning or when surfaces are shaded.

  - Do not install stain if rain is predicted within 24 hours after installation.

  - Substrates shall be uniformly dry, and free of standing water.

PART 2:  PRODUCTS

2.1  Acceptable Manufacturer

- Rhino Linings Corporation, 9747 Businesspark Avenue, San Diego, CA 92131   
Phone: 1-800-422-2603, Fax:  858-450-6881 Web: www.concretesolutions.com.

SPECIFIER NOTE:  Delete one of the following two paragraphs; coordinate with requirements of Division 1 on product options and substitutions.

- Substitutions: Not permitted.

- Requests for substitutions will be considered in accordance with provisions of Section 01 60 00.

SPECIFIER NOTE:  Edit the following paragraphs as required for the project. Delete those not required.

2.2  Stain Materials

- Stain: Chemically reactive penetrating stain designed for permanently color concrete [floors] [pavements].

- Product: [Concrete Solutions Acid Stain]

- Colors: [As selected by Architect] [_______] from manufacturer's full range.

SPECIFIER NOTE: Delete subparagraph above if colors are selected and indicate Concrete Solutions Acid Stain color name in subparagraph below. Add a schedule if multiple colors are required. Delete subparagraph below if colors are not selected.

  - Colors:  Provide the following color[s]:  [_______]

- Water:  Potable.

2.3  Sealing Materials

- Clear, Solvent-Borne, Membrane-Forming Sealing Compound: ASTM C 309, non-yellowing, VOC-compliant, high-gloss, clear liquid.

- Product: [Concrete Solutions Stamped Concrete Sealer  or Concrete Solutions Acrylic Urethane for interior or exterior applications.]

- Product:  [Concrete Solutions Sealcoat 1000 or Acrylic Urethane or WB Epoxy Clear for indoor applications only].

SPECIFIER NOTE: Delete paragraph below if slip-resistive additive is not required for interior concrete.

- Slip-Resistive Additive: Finely graded aggregate or polymer additive designed to add to sealer for slip-resistant surface.

2.4  Mixing

- Acid Stain will achieve the darkest color when used straight out of the container.  For a lighter color, the Acid Stain can be diluted up to 20 parts with water.

PART 3:  EXECUTION

3.1 Examination

- Site Verification of Conditions:  Verify installation conditions previously established under other sections are acceptable for product installation in accordance with manufacturer's instructions.

- Examine substrate for compliance with requirements.

- Do not proceed with stained concrete installation until unacceptable conditions are corrected.

3.2   Substrate Preparation

SPECIFIER NOTE: Delete paragraph below if concrete is not new.

- Allow concrete to cure minimum 28 days before staining. Concrete Solutions Resurfacer or Spray-Top® polymer concrete can generally be stained over within 12-24 hours.

- Protect surfaces not to be stained from over-spray, run-off, and tracking.

- Clean substrates thoroughly using trisodium phosphate (TSP) and water with a scrub brush, according to manufacturer's instructions. Do not use acidic cleaners to clean substrates before staining.

- For hard troweled surfaces, open surface of substrates by sanding with 80-grit sanding disk or black scrubbing pad. Test sanding in an unobtrusive location to assure that sand and aggregate are not exposed by excessive sanding.

- Test substrates by spotting with water. If water beads, or does not penetrate surface, continue preparing substrates.

- Rinse substrates until rinse water is clean. Collect cleaning residue by wet vacuuming or squeegee to drains.

- Allow substrates to dry thoroughly prior to application of stains.

- Divide substrates into small areas by natural stopping points, such as walls and joint lines.

- Protection: Protect substrates during the construction period as follows:

  - Use safe-release blue painter's masking tape. Do not use adhesive or duct tape.

- Prevent petroleum products from staining substrates.

- Diaper hydraulic equipment.

- Do not park vehicles on substrates.

- Do not place steel reinforcing bars on substrates to avoid rust stains.

- Notify other trades of protection requirement before and after stain application.

SPECIFIER NOTE:   Delete paragraph below if scoring is not required. Select optional text for time of scoring. If only one stain color, score after staining.

- Scoring: Score concrete surfaces [before] [after] staining with diamond blades to a depth of ⅛ inch (3.2 mm). Rinse until rinse water is clean.

3.3  Staining

- Apply stain to concrete surfaces by acid-resistant sprayer or acid-resistant natural fiber brush, immediately scrubbing into surface in a random circular motion, according to manufacturer's instructions.

- Maintain a wet edge, working newly applied stain into edges of adjacent wet edges of previously treated surfaces. Maintain consistent saturation throughout application. Do not splash, drip, or puddle stain on substrates to prevent darker effects.

SPECIFIER NOTE:   Delete paragraph below if staining vertical surfaces is not required.

- Apply stain to vertical surfaces in similar manner, from bottom working upward, avoiding excessive rundown of material on substrates to prevent darker streaks.

- After initial application of stain has reacted 4 hours minimum, test surface to determine if sufficient color has been applied to match field samples.

        - Remove residue from small section by wet scrubbing and rinsing.

        - If test indicates color is not sufficient, apply additional stain, allow to dry, and retest.

- When color is sufficient, neutralize stain by mopping with a solution of 10 parts water to 1 part household ammonia. Remove stain residue by wet scrubbing with water and a stiff, acid-resistant brush. Do not use soap. Rinse until rinse water is clean.

- Collect rinse water by vacuuming or absorbing with inert material. Dispose of stain residue, rinse water, and absorbent materials legally.

3.4  Sealing

- Sealer Application: After stained and rinsed concrete has thoroughly dried, uniformly apply sealer in continuous operation by sprayer or short nap roller according to manufacturer's instructions. After initial application is dry and tack free, apply a second coat.  Do not over apply or apply in a single heavy coat.

SPECIFIER NOTE: Delete subparagraphs below for interior concrete. For interior applications subject to wetting, consider slip-resistant floor wax over sealer.

  - Thoroughly mix slip-resistant additive in sealer according to manufacturer's instructions. Stir occasionally to maintain uniform distribution of additive.

  - Verify adequacy of slip resistance before opening up surfaces to traffic.

3.11  Cleaning, Protection & Repair

- Clean spillage and soiling from adjacent construction according to manufacturer's instructions.

- Protect stained concrete from damage or deterioration until date of substantial completion.

- Remove construction debris from project site in accordance with provisions outlined in Division 1.

END OF SECTION