Concrete Solutions® ¼” Stamping Overlay

Note: These specifications were current at the time of publication but are subject to change without notice. Please confirm the accuracy of these specifications with the manufacturer and / or distributor prior to installation. Specification writer shall choose the most appropriate section that applies to a given scope of work.

SECTION 03 35 19 COLORED CONCRETE FINISHING

SECTION 03 35 33 STAMPED CONCRETE

SECTION 03 53 00 CONCRETE TOPPING

SECTION 09 97 26	CEMENTITIOUS COATINGS

SECTION 32 01 26 RIGID PAVEMENT REHABILITATION

SECTION 32 13 16 DECORATIVE CONCRETE PAVING

SPECIFIER NOTE:  This product guide specification is written according to the Construction Specifications Institute (CSI) Format, including MasterFormat, SectionFormat, and PageFormat, as contained in the CSI Manual of Practice.

This section must be carefully reviewed and edited by the Architect to meet the requirements of the project and local building codes. Coordinate this section with other specification sections and drawings.

This guide specification is intended to be used by a qualified construction specifier. It should not be used without appropriate modifications. Notes for review by specifier begin with “SPECIFIER NOTE.” Optional text requiring a selection is enclosed within brackets, e.g., “Color shall be [white] [tan].” Items requiring specifier input are indicated by a blank line enclosed within brackets, e.g., “Color: [_______].” Delete all italicized “Specifier Notes” and non-applicable optional text in final specification.

This section is based on systems manufactured by Rhino Linings Corporation, 9747 Businesspark Avenue, San Diego, CA 92131 Telephone: 1-800-422-2603, FAX 858-450-6881, www.concretesolutions.com. For assistance with specific product applications, please contact the manufacturer.   Contact the manufacturer for additional information and for assistance in editing this section for your specific application.

PART 1:   GENERAL

  - Section Includes

SPECIFIER NOTE:  Edit the following list as required for the project. Delete optional text below for exterior concrete pavement or interior concrete floor that is not required.

- Cementitious stampable overlays for concrete [pavement] [floor].

- Cementitious stampable overlays for stained decorative concrete [pavement] [floor].

1.2   Related Sections

SPECIFIER NOTE:  Edit the following list of related sections as required for the project. List other sections with work directly related to this section as required.

- Section 32 13 13 – Concrete Paving (for cast-in-place concrete pavement with cementitious stampable overlays)

- Section 09 61 19 – Concrete Staining (for staining cementitious stampable overlays)

- Section 03 35 20 – Chemically Stained Concrete  (for staining cementitious stampable overlays)

- Section 03 30 00 - Cast-In-Place Concrete  (for interior concrete with cementitious stampable overlays)

1.3  Submittals

- Submit according to Section 01 33 00 - Submittal Procedures.

- Product Data: For each product indicated submit manufacturer's product data, including installation instructions.

- Samples: Submit manufacturer’s standard color chart for selection purposes and selected colors for verification purposes.

- Sample Panels: [2 by 2 feet (610 by 610 mm)] [_______], to demonstrate finish, color, and texture of cementitious stampable overlay.

- Qualification Data: For installer and manufacturer specified in Quality Assurance Article, including names and addresses of completed projects, architects, and owners.

1.4  Quality Assurance

- Manufacturer Qualifications: Company specializing in manufacturing products specified in this section with minimum three years documented experience.

- Installer Qualifications: Minimum two years documented experience with projects of similar scope and quality.

SPECIFIER NOTE:  Delete paragraph above or below.

- Installer Qualifications: Trained or approved by Manufacturer of cementitious stampable overlay systems.

- Material Source Limitations:  Obtain products from same source throughout project.

SPECIFIER NOTE:  For large projects or where color and appearance are critical, include provisions for a field sample to demonstrate range of finishes and workmanship, including sealing procedures. Approved field samples set quality standards for comparison with remaining work.

- Field Samples:  Locate at site and obtain approval before start of final work.

  - Field samples shall be minimum [4 by 4 feet (1.2 by 1.2 m)] [_______].

  - [Remove field samples when directed.] [Approved field samples may become part of the completed work if undisturbed at completion of project.]

SPECIFIER NOTE:  Delete paragraph below if pre-installation conference is not required.

- Pre-installation Conference: Conduct conference at site to comply with requirements of Section 01 31 19 – Project Meetings.

1.5  Delivery, Storage and Handling

- Comply with manufacturer's recommendations for delivery, storage and handling.

- Deliver materials to site in manufacturer’s original, unopened packaging, with labels clearly identifying product name, manufacturer, and location of installation. Upon delivery, materials shall be inspected for damage. Defective materials shall not be used.

- Storage: Store materials in a clean, dry indoor area in accordance with manufacturer’s instructions. Keep temporary protective coverings in place.

- Handling: Handle products according to manufacturer’s printed instructions.

1.6  Project Conditions

- Environmental Requirements: Comply with cementitious stampable overlay manufacturer's instructions.

  - Do not apply overlay cementitious topping if air temperature and concrete substrate temperature are not between 45 and 85 degrees Fahrenheit before and during installation.

  - In hot weather, install cementitious stampable overlay in early morning or when surfaces are shaded.

  - Keep bagged products out of sunlight. Use cool water; do not use water from hot watering hoses.

  - Protect cementitious stampable overlay from rain for 24 hours.

  - In windy weather, protect adjacent construction from over-spray during application of sealers.

PART 2:  PRODUCTS

2.1 Acceptable Manufacturer

- Rhino Linings, 9747 Businesspark Avenue, San Diego, CA 92131   
Phone: 1-800-422-2603, Fax:  858-450-6881 Web: www.concretesolutions.com.

SPECIFIER NOTE:  Delete one of the following two paragraphs; coordinate with requirements of Division 1 on product options and substitutions.

- Substitutions: Not permitted.

- Requests for substitutions will be considered in accordance with provisions of Section 01 60 00.

SPECIFIER NOTE:  Edit the following paragraphs as required for the project.  Delete those not required.

2.2   Cementitious Stampable Overlay Materials

- Concrete Solutions ¼” Stamping Mix:  Polymer-modified cementitious stampable overlay designed for texturing stable, non-moving concrete [floors] [pavements].

- Primer: [Concrete Solutions MRB Primer over unsealed concrete].

- Water:  Potable.

SPECIFIER NOTE: Delete Article below if cementitious stampable overlay will not be integrally colored.

2.3  Integrally-Colored Overlay Materials

- Concrete Solutions Integral Color Pak: factory-measured powdered mix, consisting of nonfading finely ground synthetic mineral-oxide coloring pigments and water reducing wetting agent.

- Colors: As selected by [Architect] [________].

SPECIFIER NOTE: Delete subparagraph above if colors are selected and indicate Concrete Solutions Integral Color Pak color name in subparagraph below. Add a schedule if multiple colors are required. Delete subparagraph below if colors are not selected.

- Color: Concrete Solutions Integral Color Pak [________].

SPECIFIER NOTE: Delete Article below if cementitious stampable overlay will not be stained.

2.4  Stain Materials

- Penetrating Reactive Stain:  As specified in Section 03 35 20 – Chemically Stained Concrete.

SPECIFIER NOTE: Delete Article below if cementitious stampable overlay will not be stamped.

2.5  Imprinting Tools

- Stamp Mats: Concrete Solutions semi-rigid polyurethane mats with projected texture and ridged underside capable of imprinting texture and joint patterns to plastic cementitious stampable overlay. Include texture skins matching stamp mat textures for texturing areas that cannot be reached with stamping mats.

- Pattern: As selected by [Architect] [________].

SPECIFIER NOTE: Delete subparagraph above if patterns are selected and indicate pattern name in subparagraph below. Add a schedule if multiple patterns are required. Delete subparagraph below if patterns are not selected.

- Pattern: [________].

- Accessory Stamp Tools:  Concrete Solutions aluminum detailing tools capable of imprinting joints and dressing stamped joints of plastic cementitious stampable overlay.

SPECIFIER NOTE: Delete Article below if cementitious stampable overlay will not be stamped.

2.6  Release Agents

- Concrete Solutions Liquid Release Agent: Clear, evaporating formulation that facilitates release of stamp mats and texture skins from cementitious stampable overlay.

- Concrete Solutions Antiquing Color Powder: Factory-packaged, non-fading finely-ground, streak free, colored powder that facilitates release of stamps and texture skins from cementitious stampable overlay and imparts a secondary accent color.

  - Colors:  As selected by [Architect] [________].

SPECIFIER NOTE: Delete subparagraph above if colors are selected and indicate Concrete Solutions Antiquing Color Powder color name in subparagraph below. Add a schedule if multiple colors are required. Delete subparagraph below if colors are not selected.

  - Colors:  Concrete Solutions Antiquing Color Powder [________].

2.7  Sealing Materials

- Concrete Solutions Stamped Concrete Sealer: Clear, solvent-borne, membrane-forming sealing compound: non-yellowing, VOC-compliant, high-gloss, clear liquid.

SPECIFIER NOTE: Delete paragraph below if slip-resistive additive is not required for interior concrete.

- Slip-Resistive Additive: Finely graded aggregate or polymer additive designed to add to sealer for slip-resistant surface.

2.8  Mixing

- Mix materials in accurate proportions and according to manufacturer's instructions.

- Bulk Mixing: For machine mixing of cementitious stampable overlay, use a paddle mortar mixer.

SPECIFIER NOTE: Delete paragraph below if cementitious stampable overlay will not be integrally colored.

- Add Concrete Solutions Integral Color Pak to water and then mix with cementitious stampable overlay according to manufacturer's instructions.

PART 3:  EXECUTION

3.1 Examination

- Site Verification of Conditions:  Verify installation conditions previously established under other sections are acceptable for product installation in accordance with manufacturer's instructions.

- Examine substrate for compliance with requirements.

- Do not proceed with cementitious stampable overlay installation until unacceptable conditions are corrected.

3.2   Substrate Preparation

- Map out locations of existing control joints before installation of cementitious stampable overlay.

- Thoroughly clean substrate using high-pressure water or trisodium phosphate (TSP) and water with a scrub brush, then rinse thoroughly. Remove potential bond breakers, such as grease, oil, silicone, paint, sealant, curing and sealing compounds, drywall taping compound, etc.

- For painted, sealed, or overly slick hard-troweled concrete substrates, mechanically abrade surfaces by sanding, scarifying, or shot blasting to allow for proper bonding.

- Remove weak, delaminated, or unsound concrete substrates.

SPECIFIER NOTE: Delete optional text below if concrete does not require patching.

- Patching: Fill chips, pits, and cracks prior to application of cementitious stampable overlay with the Concrete Solutions Patching Mix in lifts up to 1/2 inch. For small holes and spalls that are deeper than ½ inch make a slurry of Concrete Solutions “Powder” Polymer Concrete mixed with water, cement and sand from your local area.

- Allow surfaces to dry thoroughly prior to application of primer.

3.3  Priming Substrates

- Apply the appropriate primer to the surface and allow to dry for 3 hours.

- Apply an even squeegee of the Concrete Solutions “Powder” Polymer Concrete bond coat less than 1/16” using a special metal edged squeegee or hand trowel. Protect adjacent surfaces from overspray or splash.

- Do not allow the bond coat to dry. Immediately apply the ¼” Stamp Mix.

- Prevent contamination of primed surfaces by dirt or other deleterious materials or conditions.

3.4  Trowel- Applied Cementitious Stampable Overlay Application

SPECIFIER NOTE: Delete optional text below if cementitious stampable overlay will not be stamped.

    - Trowel Application: Distribute Concrete Solutions ¼” Stamp Mix then use a gauge rake to quickly spread the stamping mix 3/8” thick over the wet bond coat. Then use a concrete fresno to smooth out the surface.

    - Maintain a wet edge when installing cementitious stampable overlay to avoid cold joints.

    - Do not overwork material with trowel or fresno. If mix becomes sticky, lightly spray the surface with water.

    - Clean tools frequently to avoid build up of overlay materials.

    - When installation requires multiple pours over a common concrete substrate area, protect adjacent prepared concrete substrates from release agents.

3.5  Stamping

- Stamp overlay surfaces according to manufacturer's instructions. Plan stamp layout prior to application of stamps.

- Liquid Release Agent Application: Apply a liberal coat of Liquid Release Agent to cementitious stampable overlay when set sufficiently to achieve a clean impression.

- Stamping:

  - Stamp perimeter of pour using texture skins.

  - Accurately align stamp mats in sequence and tamp into cementitious stampable overlay to produce imprint pattern, texture, and depth of imprint, according to manufacturer's instructions. Remove stamps from cementitious stampable overlay immediately.

  - Stamp edges and surfaces unable to be imprinted with stamp mat with texture skins.

  - Use stamp tools to imprint grout lines at edges and surfaces unable to be imprinted with stamp mats.

3.6  Joints

- Recut existing control joints before cracking occurs, generally within 12 to 24 hours after placement at 70 degrees Fahrenheit.

SPECIFIER NOTE: Delete optional text below if antiquing color is not required for stamped overlay or if cementitious stampable overlay is stained.

3.7  Antiquing

- Mix 2-4 ounces of Antiquing Color Powder of the color desired to 1 gallon of Liquid Release Agent.

- Start by spraying a thin even coat ahead of the stamps.

- After stamping and moving a few stamps, spray more colored Liquid Release Agent and allow it to puddle in the low areas of the texture, creating a natural-looking color effect.

- Before spraying the colored Liquid Release Agent, always shake the sprayer to be sure the color is evenly mixed.

- If you get too much color on the surface, use a rag to gently clean it off while it is still wet or spray clear Liquid Release Agent over it to move it around and lighten the color.

3.8  Staining

SPECIFIER NOTE: Delete optional text below if cementitious stampable overlay will not be stained.

- Apply stain as specified in Section [09 61 19 – Concrete Staining] [Section 03 35 20 – Chemically Stained Concrete].

3.9  Sealing

SPECIFIER NOTE: Delete optional text below if cementitious stampable overlay is stained.

- Sealer Application: Apply uniformly in continuous operation by sprayer or short nap roller according to manufacturer's instructions. After initial application is dry and tack free, apply a second coat.  Do not over apply or apply in a single heavy coat.

SPECIFIER NOTE: Delete paragraph above if antiquing release agent is used. Delete paragraph below if antiquing agent is not used.

- Sealer Application: Apply final coat of Concrete Solutions Stamped Concrete Sealer uniformly in continuous operation by sprayer according to manufacturer's instructions.

SPECIFIER NOTE: Delete subparagraphs below for interior concrete. For interior applications subject to wetting, consider slip-resistant floor wax over sealer.

  - Thoroughly mix slip-resistant additive in sealer according to manufacturer's instructions. Stir occasionally to maintain uniform distribution of additive.

  - Verify adequacy of slip resistance before opening up surfaces to traffic.

3.10  Cleaning, Protection & Repair

- Repair damaged cementitious stampable overlay according to manufacturer's instructions.

- Clean spillage and soiling from adjacent construction according to manufacturer's instructions.

- Protect cementitious stampable overlay from damage or deterioration until date of substantial completion.

- Remove construction debris from project site in accordance with provisions outlined in Division 1.

END OF SECTION